## Slide 1
Dieless Deposition Manufacturing
Instructions
Last updated: May 23, 2013

## Slide 2: Introduction/Summary
1
Print finger frames via 3D printer
Seal/tape finger frames
Prepare rubber urethane mixtures
Pour joint flexure urethanes
Pour finger pad urethanes
Wait for urethanes to cure (24-48 hours)
Cut away sacrificial walls
Step-by-step video also available at: www.youtube.com/watch?v=dEJJMax7hs0

## Slide 3: Sealing
2
Remove all support material prior to pouring
DO NOT pour on top of support material
  Urethanes will leak through support material
Use tape to seal bottom of finger molds
  Most adhesives will suffice
  Some leakage is expected, not critical
  Heating duct tape (and more rigid tapes) are preferred

## Slide 4: Selected Urethanes
3
Finger Joints:
PMC-780 Urethane [link]
  Two-part rubber compound
  PMC-790 too stiff for general use cases
  Demold time: 48 hours
Finger Pads:
Vytaflex-20/30 Urethane [link]
  Two part urethane rubber
  PMC-780 and other Vytaflex options can act as suitable replacements
  Demold time: 16 hours
Commercial rubber urethanes are mixed just like two-part epoxy
Mix according to ratios in instructions, either by volume or mass
  Mass scale will need 0.1g precision due to small quantity that is mixed

## Slide 5: Degassing (Optional)
4
Why Degas?
More evenly distributed bubble/imperfection formation
Higher density
Higher stiffness
Higher degree of manufacturing repeatability
Degas
No Degassing
Solutions:
Low vacuum in dessicator (see figure to the left)
  Leave mixed urethane in vacuum for < 2 min
  Urethane will quickly rise and fall
Consider alternative urethanes that set more quickly
  Alternative urethanes from those listed in this guide have not been tested in OpenHand projects

## Slide 6: Pouring
5
Pour from as high and with as thin a stream as possible
Pour more than necessary
  Excess material can be cut off and removed later
Less viscous urethanes have higher chances of leakage
  Can wait ~15 min for urethanes to become more viscous and easier to pour if desired
Tips/suggestions for pouring also available via the urethane distributor at www.smooth-on.com

## Slide 7: Wall Removal
6
ABS frame ~0.7-1.0 mm thick
  Bandsaw or file used to cut out frame elements
  Compliance of joints/pads minimizes damage if cut is excessive
  Can partially cut and then “snap” frame elements apart
File, blade, or belt sander can be used to smooth, file-down excess ABS or urethane material